## Slide 1
Hardness defect problem of heat-treated products
(熱処理品の硬さ不良問題)
16/MAY/24
Report No：ADSI 24-006
TECHNICAL SECTION (Takayuki Eto )

## Slide 2
１．Occurrence Status (発生状況)
When the DHA-WORLD mold manufactured by your company was heat treated with ADSI, an event occurred where the hardness was significantly lower than the hardness standard (47-49HRC).
(貴社にて製造したDHA-WORLD製金型をADSIで熱処理したところ、硬さ規格(47-49HRC)に対し、
大きく下回る事象が発生)
We have investigated the cause of the occurrence and will report it here.
(発生原因について調査しましたので、報告致します)

## Slide 3
２．Process (工程)
Process | Date | Pcs | Remarks
Order | 2024/4/17 | 2 | Material：DHA-WORLD Order Size：56x80x121
Cutting | 2024/4/17 | 2 | Stock size used：Stok A [60x115x153] Stok B [60x130x155]
Milling | 2024/4/18 | 2 | Process：6W
Delivery | 2024/4/20 | 2 | 
HT | ー | 2 | HT processing (At Kanetsu) 【Request hardness :47-49HRC】 ・Hardness of both is NG
 | ー | 1 | Re-HT processing (At Kanetsu) ・Hardness OK
 | 2024/5/7 | 1 | Re-HT processing (At ADSI) Heat treatment conditions H:1030℃、T:500℃ ・Hardness NG (35.5HRC)
Table. Process details
Low hardness mold

## Slide 4
[Stok A] Size:60x115x153
[Stok B] Size:60x115x153
３．Inventory & Cutting (在庫＆切断)
Material ：DHA-WORLD
Order Size：56x80x121 (2pcs)
115
153
60
121
80
130
155
60
80
All rest stock is scrapped.
(残った端材はすべて屑化)
Rest stock is kept(60x67x130)
(残った端材は保管(60x67x130))
Scrapped
Scrapped
Rest stock

## Slide 5
４．Chemical analysis results (化学分析結果)
 | Measuring element |  |  |  |  |  |  | 
 | Si | Mn | P | S | Ni | Cr | Mo | V
Low hardness mold | 0.296 | 1.62 | 0.0143 | 0.0218 | 0.064 | 2.33 | 0.265 | 0.098
Stock B (rest stock) (60x67x130) | 0.296 | 1.64 | 0.0136 | 0.0142 | 0.064 | 2.34 | 0.264 | 0.099
DHA-WORLD | 0.47 | 0.71 | 0.011 | 0.001 | 0.07 | 5.54 | 1.24 | 0.57
PX4 | 0.24 | 1.60 | 0.011 | 0.01 | 0.06 | 2.20 | 0.37 | 0.11
P20 | 0.32 | 1.39 | － | － | 0.12 | 1.92 | 0.19 | －
・Both low hardness mold and stock B (rest stock) have chemical composition similar to PX4.
(低硬度型、ストックB(端材)ともにPX4に近しい化学組成)
・Low hardness mold and stock B(rest stock) were not DHA-WORLD but PX4 equivalent material
(低硬度型とストックB(端材)はDHA-WORLDではなく、PX4相当材であった)
Table. Chemical analysis results
・It is assumed that the low hardness problem occurred with the ordered product cut from stock B.
(ストックBから採取したオーダー品で低硬度問題が発生したと推察される)

## Slide 6
５．Rest stock history (端材履歴)
No. | Date | Customer | Stok Size | Order Size
① | 2023/ 9/26 | A | 165x518x660 | 155x159x516
② | 2023/ 9/27 |  | 165x507x518 | 133x142x417
③ | 2023/ 9/27 |  | 165x345x518 | 155x159x516
④ | 2023/10/16 | B | 150x165x518 | 111x156x176
⑤ | 2023/10/16 |  | 125x165x303 | 76x76x107
⑥ | 2024/ 2/ 1 | C | 130x160x190 | 105x108x153
➆ | 2024/ 4/17 | CSM | 60x130x155 | 56x80x121
518
660
159
165
①
518
507
142
165
②
518
345
159
165
③
60
130
155
80
➆
60
130
67
190
130
160
108
⑥
303
125
165
107
⑤
518
150
165
176
④
Table. Stok B rest stock history

## Slide 7
６．Presence of hardness defect problem (硬さ不良問題の有無)
No. | Date | Customer | Stok Size | Order Size | Hardness defect problem
① | 2023/ 9/26 | A | 165x518x660 | 155x159x516 | No
② | 2023/ 9/27 |  | 165x507x518 | 133x142x417 | 
③ | 2023/ 9/27 |  | 165x345x518 | 155x159x516 | 
④ | 2023/10/16 | B | 150x165x518 | 111x156x176 | 
⑤ | 2023/10/16 |  | 125x165x303 | 76x76x107 | 
⑥ | 2024/ 2/ 1 | C | 130x160x190 | 105x108x153 | 
➆ | 2024/ 4/17 | CSM | 60x130x155 | 56x80x121 | Yes
・No. ①～⑥ Delivered products have no hardness problems during subsequent heat treatment.
(No.①～⑥納入品で、その後の熱処理で硬さ不良問題発生無し)
・Hardness defect problem occurred only in No.➆
(No.➆のみ硬さ不良問題発生)
・No.⑥ It is possible that wrong material occurred during the process after cutting.
(No. ⑥切断以降の工程で異材が発生した可能性が考えられる)
Table. Stok B rest stock history

## Slide 8
７．Estimated cause of occurrence (推定発生原因)
Table. Cutting history
No. | Date | Customer | Stok Size | Order Size
⑥ | 2024/ 2/ 1 | C | 130x160x190 | 105x108x153
➆ | 2024/ 4/17 | CSM | 60x130x155 | 56x80x121
Table. Stok B rest stock history
Date | Cutting machine | Start | Finish | Material | Order Size | Pcs
2024/2/1 | C12 | 3:51 AM | 4:09 AM | SKD11 | 25x105x120 | 1
 |  | 8:30 AM | 8:45 AM | NAK80 | φ180x55 | 1
 |  | 8:45 AM | 9:01 AM | PX4 | 73x135x125 | 2
 |  | 9:01 AM | 9:15 AM | PX4 | 62x125x135 | 2
 | C13 | 2:00 AM | 3:09 AM | GFA | 15x270x510 | 1
 |  | 8:30 AM | 10:12 AM | DHA-WORLD | 105x108x153 | 1
 |  | 10:12 AM | 11:21 AM | PAC5000 | 30x200x425 | 1
 | C14 | 3:27 AM | 7:11 AM | DHA1 | φ585x107 | 1
 |  | 8:30 AM | 5:30 PM | S50C | 54x80x240 | 30
⑥
The worker who was cutting No.⑥ mixed the material with other materials that were cut using
the cutting machine that he was in charge of at the same time.
(No.⑥切断した作業者が同時に担当していた切断機で切断した他鋼種と混在した)
⇒There is PX4 in the cutting history for the same time as the target product (At C12 cutting machine)
(対象品と同時間の切断履歴にPX4有り(C12切断機))
◆There is a possibility that materials were mixed at this time.
(この時に材料が混在した可能性が有り)

## Slide 9
Two types of cut rest stock were temporarily no display and then displayed the wrong material name.
(2鋼種の切断後の端材が、一時的に無表示のまま置かれ、その後間違って鋼種名が表示された)
DHA-WORLD
DHA-WORLD
Cutting
After cutting
Write
PX4
PX4
Cutting
After cutting
Write
Temporarily no display
(一時的に無表示状態となる)
Incorrect display
(表示間違い)
７．Estimated cause of occurrence (推定発生原因)
DHA-WORLD
PX4
Mixed
(混在)
Cut
Cut

## Slide 10
・Always displayed
(常に表示されている)
・Do not create a state where
there is no display
(無表示状態をつくらない)
８．Measures (対策)
（１） Measures to prevent wrong material by changing the material display method
(材料表示方法変更による異材防止対策)
DHA-WORLD
DHA-WORLD
Cutting
After cutting
Write
Temporarily no display
(一時的に無表示状態となる)
DHA-WORLD
Write & Cutting
After cutting
Write the material name before cutting
(切断前に鋼種名を記入する)
DHA-WORLD
DHA-WORLD
Displayed even after cutting
(切断後も表示有り)
Before
Improvement
Write after cutting
(切断後に記入)
Cut
Cut

## Slide 11
８．Measures (対策)
（２） Measures to prevent wrong material by using a special box for small items.
(小物用専用BOX使用による異材防止対策)
Before
Improvement
DHA1
PAC5000
PAC5000
DHA1
Rest stocks made of different materials are placed on a trolley as is.
(材質の異なる端材がそのまま台車に乗っている)
Manage each material using a dedicated box for small items
(材料別に小物専用BOXを使用して管理する)

## Slide 12
７．Estimated cause of occurrence (推定発生原因)
（１） No.➆When cutting, other materials cut before and after were mixed together.
(No.➆切断時に、前後に切断した他鋼種と混在した)
⇒There is no PX4 in the cutting history before and after the target product.
(対象品前後の切断履歴にPX4無し)
◆No possibility of mixed （混在する可能性無し）
Table. Cutting history
No. | Date | Customer | Stok Size | Order Size
⑥ | 2024/ 2/ 1 | C | 130x160x190 | 105x108x153
➆ | 2024/ 4/17 | CSM | 60x130x155 | 56x80x121
Table. Stok B rest stock history
Date | Cutting machine | Start | Finish | Material | Order Size | Pcs
2024/4/17 | C11 | 8:30 AM | 2:30 PM | SKD61 | φ95x92L | 5
 |  | 2:30 PM | 4:51 PM | DC11 | φ242x42L | 1
 |  | 4:51 PM | 5:27 PM | DHA-WORLD | 61x85x126 | 2
 |  | 8:00 PM | 9:08 PM | SCM440Q | φ180x70L | 2
 |  | 9:08 PM | 10:17 PM | SCM440Q | φ180x35L | 2
 |  | 10:17 PM | 10:40 PM | P20 | 35x155x155 | 2
 |  | 10:40 PM | 11:12 PM | S50C | 70x155x155 | 2
 |  | 11:12 PM | 12:06 AM | DC53 | 40x100x340 | 1
➆

## Slide 13
７．Estimated cause of occurrence (推定発生原因)
（２） The worker who was cutting No.➆ mixed the material with other materials that were cut using
the cutting machine that he was in charge of at the same time.
(No.➆切断した作業者が同時に担当していた切断機で切断した他鋼種と混在した)
⇒There is no PX4 in the cutting history for the same time as the target product.
(対象品と同時間の切断履歴にPX4無し)
◆No possibility of mixed （混在する可能性無し）
Table. Cutting history
No. | Date | Customer | Stok Size | Order Size
⑥ | 2024/ 2/ 1 | C | 130x160x190 | 105x108x153
➆ | 2024/ 4/17 | CSM | 60x130x155 | 56x80x121
Table. Stok B rest stock history
Date | Cutting machine | Start | Finish | Material | Order Size | Pcs
2024/4/17 | C10 | 2:46 PM | 3:02 PM | SKD61 | φ60x80 | 1
 |  | 3:02 PM | 5:02 PM | DC53 | φ90x2565 | 1
 |  | 8:00 PM | 8:11 PM | S45C | φ75x60 | 1
 | C11 | 2:30 PM | 4:51 PM | DC11 | φ242x42L | 1
 |  | 4:51 PM | 5:27 PM | DHA-WORLD | 61x85x126 | 2
 |  | 8:00 PM | 9:08 PM | SCM440Q | φ180x70L | 2
 | C12 | 3:37 PM | 4:22 PM | DH31-EX | 125x376x381 | 1
 |  | 4:22 PM | 6:02 PM | DHA-WORLD | 87x257x297 | 2
 |  | 8:00 PM | 9:40 PM | DHA-WORLD | 87x257x297 | 2
➆

## Slide 14
７．Estimated cause of occurrence (推定発生原因)
（３） No.⑥ When cutting, other materials cut before and after were mixed together.
(No.⑥ 切断時に、前後に切断した他鋼種と混在した)
⇒There is no PX4 in the cutting history before and after the target product.
(対象品前後の切断履歴にPX4無し)
◆No possibility of mixed （混在する可能性無し）
Table. Cutting history
No. | Date | Customer | Stok Size | Order Size
⑥ | 2024/ 2/ 1 | C | 130x160x190 | 105x108x153
➆ | 2024/ 4/17 | CSM | 60x130x155 | 56x80x121
Table. Stok B rest stock history
Date | Cutting machine | Start | Finish | Material | Order Size | Pcs
2024/2/1 | C13 | 2:00 AM | 3:09 AM | GFA | 15x270x510 | 1
 |  | 8:30 AM | 10:12 AM | DHA-WORLD | 105x108x153 | 1
 |  | 10:12 AM | 11:21 AM | PAC5000 | 30x200x425 | 1
 |  | 11:45 AM | 12:46 PM | SKD11 | φ180x15 | 5
 |  | 1:00 PM | 1:11 PM | DH31-S | 127x127x80 | 4
 |  | 1:11 PM | 1:23 PM | DH31-S | 127x127x75 | 4
 |  | 1:23 PM | 2:33 PM | SNCM439 | φ450x80 | 2
 |  | 2:33 PM | 3:53 PM | DC53 | φ320x50 | 2
⑥